## Slide 1
SPS MD run 6.10 – 8.10 with 25ns, 50ns and 75ns LHC beam
SPSU-team
TS-MME, AT-VAC, AB/OP-RF-BI-ABP
Results from the SPS run week 41

## Slide 2
Normalized current
Carbon
NEG
A factor of 10 lower
than the previous measurement.
The same as the previous measurement.
5 times higher than the previous measurement.
Stainless steel
Results SPS MD run week 41: 25 ns spacing LHC beam

## Slide 3
magnet on
Effect of bad vacuum?
Stainless steel
Dose [nClb]
x108
Normalized current
CARBON
Dose [nClb]
x104
Normalized current
X10-3
Dose [nClb]
x106
Normalized current
NEG
0
-50
-100
X10-3
Results of previous MD run (12.8) at 25 ns spacing for comparison

## Slide 4
Normalized current
No detectable e-cloud
Carbon
Stainless Steel
-No e-cloud effect with 50ns
- noise?
e-cloud (5 times lower current than at 25 ns)
Results SPS MD run week 41: 50 ns LHC beam
NEG
Carbon

## Slide 5
Normalized current
Stainless Steel
Carbon
NEG
No detectable e-cloud
Weak but detectable
(1000 times less than at 25 ns)
Results SPS MD run with 75 ns spacing LHC beam
E-cloud, current as for 50 ns
(5 times lower than at 25 ns)

## Slide 6
Conclusions for liners left in the SPS for 2 months:
On C:
-decrease of normalized e-cloud current at 25 ns spacing compared to previous run with same liner
No detectable current at 50 ns and 75 ns
On stainless steel
Same current as before at 25 ns spacing
5 times less current at 50 ns and 75 ns
On NEG:
-5 times more current than before at 25 ns
-not measurable at 50 ns (?)
- 10000 times less at 75 ns than at 25 ns