## Slide 1
News from aging of SPS liner samples
SEY meeting 2010-10-06
Christina Yin Vallgren

## Slide 2: Inspection of five liners extracted from the SPS
Liner | SPS operation time | δ initial
StSt (Ref) | 1 year (5 MD runs) | 2.25
C-strip | 1 year (5 MD runs) | 0.92
C-Zr | 1.5 years (9 MD runs) | 0.95
CNe64 | 3 months (2 MD runs) | 0.95
CNe65 | 3 months (2 MD runs) | 0.95

## Slide 3
C-strip
For confirming necessity of coating width
C-Zr
a-C on rough Zr coating
CNe64
a-C number 64
CNe65
a-C number 65
Stainless Steel
Reference

## Slide 4
Three New extracted liners: C-Zr, CNe64, CNe65
Chart: distance [mm]
| 0 | 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 70 | 75 | 80 | 85 | 90 | 95
CZr | 0.92 | 0.95 | 0.96 | 0.92 | 0.9 | 0.925 | 0.96 | 1.02 | 1.02 | 1.01 | 0.967 | 0.91 | 0.906 | 0.937 | 0.99 | 0.97 | 1 | 1.01 | 1.05 | 1.03
CNe64 | 0.969 | 0.965 | 0.967 | 0.958 | 0.952 | 0.948 | 0.946 | 0.941 | 0.941 | 0.932 | 0.946 | 0.952 | 0.946 | 0.947 | 0.953 | 0.96 | 0.972 | 0.985 | 1.01
CNe65 | 0.972 | 0.975 | 0.958 | 0.954 | 0.946 | 0.948 | 0.941 | 0.946 | 0.95 | 0.941 | 0.946 | 0.942 | 0.953 | 0.957 | 0.983 | 0.992 | 0.982 | 1

## Slide 5
Summary: five extracted liners
Chart: 
| 32 | 82 | 132 | 182 | 232 | 282 | 332 | 382 | 432 | 482 | 532 | 582 | 632 | 682 | 732 | 782 | 832 | 882 | 932 | 982 | 1032 | 1082 | 1132 | 1182 | 1232 | 1282 | 1332 | 1382 | 1432 | 1482 | 1532 | 1582 | 1632 | 1682 | 1732
SPS StSt Ref center part | 1.0189 | 1.2823 | 1.4961 | 1.6223 | 1.6888 | 1.7208 | 1.7257 | 1.7172 | 1.6954 | 1.6673 | 1.6355 | 1.603 | 1.5715 | 1.5409 | 1.5136 | 1.4863 | 1.4569 | 1.432 | 1.4119 | 1.395 | 1.3762 | 1.3602 | 1.3448 | 1.3283 | 1.3116 | 1.2947 | 1.2777 | 1.2611 | 1.2456 | 1.2293 | 1.2147 | 1.201 | 1.1887 | 1.1779 | 1.1684
SPS StSt Ref edge part | 1.0439 | 1.3789 | 1.5927 | 1.7352 | 1.8104 | 1.8507 | 1.863 | 1.8578 | 1.8404 | 1.8125 | 1.7803 | 1.7466 | 1.713 | 1.6805 | 1.6484 | 1.6185 | 1.5852 | 1.5604 | 1.5393 | 1.5213 | 1.5036 | 1.4878 | 1.4716 | 1.4545 | 1.4368 | 1.4155 | 1.3931 | 1.3708 | 1.3503 | 1.3321 | 1.315 | 1.2991 | 1.2846 | 1.273 | 1.2621

## Slide 6
Chart: CNe32 v.s. SPS a-C liner
| 32 | 82 | 132 | 182 | 232 | 282 | 332 | 382 | 432 | 482 | 532 | 582 | 632 | 682 | 732 | 782 | 832 | 882 | 932 | 982 | 1032 | 1082 | 1132 | 1182 | 1232 | 1282 | 1332 | 1382 | 1432 | 1482 | 1532 | 1582 | 1632 | 1682 | 1732
SPS carbon strip center part | 0.74556 | 0.66666 | 0.80983 | 0.89269 | 0.93965 | 0.96293 | 0.97181 | 0.97173 | 0.96373 | 0.95237 | 0.93997 | 0.92758 | 0.91498 | 0.90179 | 0.88972 | 0.8765 | 0.86592 | 0.85439 | 0.84342 | 0.83201 | 0.81985 | 0.80855 | 0.79714 | 0.78668 | 0.77626 | 0.7674 | 0.76017 | 0.75252 | 0.74525 | 0.73873 | 0.73185 | 0.72597 | 0.71918 | 0.71294 | 0.70622
SPS carbon strip edge part | 0.8581 | 0.69245 | 0.83754 | 0.92044 | 0.96808 | 0.99154 | 1.0005 | 0.99961 | 0.99341 | 0.98476 | 0.97284 | 0.96006 | 0.94835 | 0.93587 | 0.92446 | 0.91211 | 0.90133 | 0.88967 | 0.87919 | 0.86811 | 0.85679 | 0.84539 | 0.83496 | 0.82449 | 0.81461 | 0.80557 | 0.79718 | 0.79019 | 0.78302 | 0.77653 | 0.76859 | 0.76291 | 0.75624 | 0.74938 | 0.74309
CNe32 top initial | 0.85362 | 0.6302 | 0.76767 | 0.84961 | 0.89373 | 0.91435 | 0.92796 | 0.92954 | 0.92681 | 0.92248 | 0.91065 | 0.90724 | 0.89889 | 0.88947 | 0.88212 | 0.8689 | 0.86091 | 0.85381 | 0.84291 | 0.83353 | 0.82699 | 0.81466 | 0.80445 | 0.79785 | 0.78913 | 0.77942 | 0.77289 | 0.76688 | 0.75778 | 0.75102 | 0.744 | 0.73837 | 0.73282 | 0.72798 | 0.7236
CNe32 top 1 year in air | 0.89157 | 0.90162 | 1.0642 | 1.1587 | 1.2095 | 1.2323 | 1.2377 | 1.2311 | 1.2162 | 1.1966 | 1.1764 | 1.1531 | 1.1319 | 1.1105 | 1.0894 | 1.0697 | 1.0498 | 1.0316 | 1.0141 | 0.99756 | 0.98114 | 0.96536 | 0.94912 | 0.9335 | 0.91816 | 0.90463 | 0.89131 | 0.87833 | 0.86643 | 0.85548 | 0.84434 | 0.8339 | 0.82383 | 0.81353 | 0.80355