## Slide 1
Coatings and coating systems
Two main strategies to coat the vacuum chambers for the magnets of the SPS:
The chamber is OUTSIDE the magnet
The chamber is kept INSIDE the magnet
CHAMBER INSIDE MAGNET
Coating temperature limited to 150oC
Coating limited to shutdowns
Radiation issues
Chemical treatment limited and expensive
not necessary to open dipoles
high production rate requires large space and many coating systems
CHAMBER OUTSIDE MAGNET
coating temperature > 150oC
work independent of shutdowns
no radiation issues
easy chemical cleaning
welding/machining after coating and open/close dipole
very high production rate (~40 chambers/week with LSS system)

## Slide 2
Coatings and coating systems
Two main strategies to coat the vacuum chambers for the magnets of the SPS:
The chamber is OUTSIDE the magnet
The chamber is kept INSIDE the magnet
CHAMBER INSIDE MAGNET
CHAMBER OUTSIDE MAGNET
Magnetron sputtering (with permanent magnets)
Magnetron sputtering (with the dipole’s field)
Plasma Assisted Chemical Vapour deposition. (PACVD)
Hollow Cathode Discharge sputtering
Magnetron sputtering (magnetic field by external solenoide)

## Slide 3
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
MBB vacuum chamber
Housing vacuum chamber
External solenoide
Bottom extention with MBB crossection

## Slide 4
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Rectangular graphite cathode 60mm wide and 7400 mm long (built from 30x1000 mm pieces)

## Slide 5
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Rectangular graphite cathode 60mm wide and 7400 mm long (built from 30x1000 mm pieces)

## Slide 6
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Rectangular graphite cathode 60mm wide and 7400 mm long (built from 30x1000 mm pieces)
Very stable and uniform discharge
Substrate temperature ~230oC
Good thickness uniformity
Chart: Distance [mm]
| 0 | 3.8940000000000037 | 8.5040000000000049 | 11.562000000000006 | 14.421000000000005 | 17.346000000000004 | 21.47 | 25.707999999999988 | 29.546999999999986 | 33.518000000000001 | 37.693000000000012 | 41.555 | 45.598000000000013 | 49.624000000000002 | 49.624000000000002 | 53.764000000000003 | 57.838000000000001 | 61.763000000000012 | 65.468999999999994 | 70.149000000000001 | 73.206999999999994 | 77.557999999999993 | 81.703000000000003 | 85.6 | 89.69 | 93.575000000000003 | 97.64500000000001 | 99.264000000000024
AM | 506.475 | 558 | 706.2 | 800.125 | 863.175 | 894.825 | 953.325 | 987.375 | 986.675 | 1080 | 1021.75 | 1016.25 | 1038.75 | 1088 | 1115.25 | 1047.75 | 1002.575 | 1049 | 1066.5 | 1102.25 | 1082.5 | 1015.975 | 993.3 | 988.375 | 942.5 | 834.525 | 744.875 | 735.55

## Slide 7
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Rectangular graphite cathode 60mm wide and 7400 mm long (built from 30x1000 mm pieces)
Very stable and uniform discharge
Substrate temperature ~230oC
Good thickness uniformity
SEY~1.0 after coating. No ageing after 70 days in N2.

## Slide 8
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Rectangular graphite cathode 60mm wide and 7400 mm long (built from 30x1000 mm pieces)
Very stable and uniform discharge
Substrate temperature ~230oC
Good thickness uniformity
SEY~1.0 after coating. No ageing after 70 days in N2. NO AGEING AFTER MBB ASSEMBLING

## Slide 9
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Rectangular graphite cathode 60mm wide and 7400 mm long (built from 30x1000 mm pieces)
Very stable and uniform discharge
Substrate temperature ~230oC
Good thickness uniformity
SEY~1.0 after coating. No ageing after 70 days in N2. NO AGEING AFTER MBB ASSEMBLING

## Slide 10
Coatings and coating systems
CHAMBER OUTSIDE MAGNET:
Magnetron sputtering (magnetic field by external solenoide)
Conclusions
Coating the tubes outside the magnets works
Installation in the magnets do not pollute the chamber
The possibility to coat at high temperature is a plus
Weak point: fragile cathode
Next steps
Coat MBA tubes
Design a more robust cathode
Start the design of the large scale production system? (design office)

## Slide 11
Coatings and coating systems
CHAMBER INTSIDE MAGNET:
Magnetron sputtering with permanent magnets
Slit to insert the permanent magnetic system
Graphite cathode
Magnetic circuit and cathode erosion

## Slide 12
Coatings and coating systems
CHAMBER INTSIDE MAGNET:
Magnetron sputtering with permanent magnets
Magnetic circuit and cathode erosion

## Slide 13
Coatings and coating systems
CHAMBER INTSIDE MAGNET:
Magnetron sputtering with permanent magnets
Magnetic circuit and cathode erosion
Graphite cathodes
plasmas

## Slide 14
Coatings and coating systems
CHAMBER INTSIDE MAGNET:
Magnetron sputtering with permanent magnets
Magnetic circuit and cathode erosion
Relief
sample

## Slide 15
Coatings and coating systems
CHAMBER INTSIDE MAGNET:
Magnetron sputtering with permanent magnets
Magnetic circuit and cathode erosion
sample
Relief: fractal like: due to ion bombardment during coating?
SEY:
0.98 after coating;
1.05 after 3.5 months in lab (Al foil)
How to avoid this relief?
Avoid localized ion bombardment by displacing the magnetic system

## Slide 16
Coatings and coating systems
CHAMBER INTSIDE MAGNET:
Magnetron sputtering with permanent magnets
Conclusions
Magnetron sputtering with permanent magnets is promising
Low ageing (due to ion bombardment?)
If we master the relief, it is worth to invest in a longer prototype
Next steps
Coating with constant displacement of the magnetic system
Built and test a 1 meter long prototype
If it works, build a 6.4 meter long prototype.