## Slide 1: Analyzed Data MD runs 17.08.2011 (50ns, Q26 and Q20) 02.09.2011 (25ns, Q26, B-field)
Mauro Taborelli, Holger Neupert, Mounir Mensi

## Slide 2: Configuration E-cloud measurements SPS
E-cloud monitors with liners in sextant 5 since 05.07.2011:
CNe13
3y in SPS
StSt 9
SC#8
CNe#87
Half coated
XSD1
XSD2
ECEX
XSDNEG

## Slide 3: 17.08.2011 (50ns, Q26 and Q20)
No significant differences between Q26 and Q20 settings on stainless steel e-cloud monitor. Attention: Q26 3 batches, Q20 2 batches

## Slide 4: 17.08.2011 (50ns, Q26 and Q20)
Appearance of ecloud with Q26 and Q20 optics
Show pictures under: G:\Divisions\EST\Groups\SM\ThinFilms\DataFiles\SPS_E_Cloud_Data\MD_20110817\movie
No differences in location and size of the e-cloud for Q26 and Q20 settings

## Slide 5: 02.09.2011 (25ns, Q26, B-field)
All monitors together: increasing e-cloud with decreasing B-field for stainless steel and half coated liner

## Slide 6: 02.09.2011 (25ns, Q26, B-field)

## Slide 7: 02.09.2011 (25ns, Q26, B-field)

## Slide 8: 02.09.2011 (25ns, Q26, B-field)

## Slide 9: 02.09.2011 (25ns, Q26, B-field)
Appearance of ecloud with Q26 and changing magnetic dipole field
Show pictures under: G:\Divisions\EST\Groups\SM\ThinFilms\DataFiles\SPS_E_Cloud_Data\MD_20110902\movie
Stainless steel and half coated with similar patterns
Carbon coated liners also similar

## Slide 10: 02.09.2011 (25ns, Q26)
Stainless steel and half coated liner condition similarly, same slope
Beam: only 3 batches of 72 bunches 25ns, during 6.5 hours

## Slide 11: 17.08.2011 (50ns, Q26 and Q20)

## Slide 12
ECM current/BCT as a function of B field (3 batches, 25 ns)
Chart: 
| 0.1 | 0.2 | 0.30000000000000016 | 0.4 | 0.5 | 0.60000000000000031 | 0.70000000000000029 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9000000000000001 | 2 | 2.1 | 2.2000000000000002 | 2.5 | 3 | 3.5 | 5 | 5.5 | 6 | 6.5 | 7 | 8 | 9 | 10 | 12 | 15 | 20 | 25
 | -95226 | -76667.68 | -311724.88 | -505505.76 | -650116.16 | -678111.52 | -738318.48 | -774251.44 | -825053.28 | -825053.28 | -845756.48 | -837714.88 | -848345.84 | -849332 | -838185.28 | -796021.28 | -796021.28 | -789623.44 | -756869.44 | -722107.28 | -700945.52 | -645615.44 | -537686.08 | -454436 | -226892.48 | -290718.48 | -296408.88 | -288176.8 | -283690.72 | -259693.84 | -247004.64 | -237510.48 | -215542.56 | -203762.48 | -181178.64 | -152925.76 | -97535.52