## Slide 1
Summary of SPS MDrun week35
SPS-U meeting 2010-09-23
Christina Yin Vallgren
SPS-U team

## Slide 2: Summary
3 Nov 09:00 – 4 Nov 07:00
3 Nov 11:00 – 3 Nov 20:00: 1-4x36, 50 ns
3 Nov 21:00 – 4 Nov 07:00: 1-4x72, 25 ns
ECM liners: DLC, CNe70 half coated, CNe13 and Ref StSt.
MBB magnets: 3 new coated MBB
Chart: 
| 32 | 82 | 132 | 182 | 232 | 282 | 332 | 382 | 432 | 482 | 532 | 582 | 632 | 682 | 732 | 782 | 832 | 882 | 932 | 982 | 1032 | 1082 | 1132 | 1182 | 1232 | 1282 | 1332 | 1382 | 1432 | 1482 | 1532 | 1582 | 1632 | 1682 | 1732
DLC from Kato 1 | 1.0487 | 1.4811 | 1.7655 | 1.85 | 1.8355 | 1.7777 | 1.7001 | 1.6151 | 1.5288 | 1.4451 | 1.3702 | 1.3045 | 1.2476 | 1.1978 | 1.1542 | 1.1154 | 1.0777 | 1.0479 | 1.0209 | 0.99782 | 0.97415 | 0.95046 | 0.92628 | 0.90118 | 0.88009 | 0.86274 | 0.84704 | 0.83145 | 0.81617 | 0.80101 | 0.78801 | 0.77514 | 0.76268 | 0.75134 | 0.74139
DLC from Kato 2 | 1.035 | 1.3512 | 1.6913 | 1.7236 | 1.7106 | 1.6517 | 1.5738 | 1.4907 | 1.4118 | 1.3391 | 1.2731 | 1.214 | 1.1641 | 1.1201 | 1.081 | 1.0462 | 1.0155 | 0.98788 | 0.96399 | 0.9406 | 0.91924 | 0.89831 | 0.87832 | 0.86094 | 0.84529 | 0.8299 | 0.81659 | 0.80468 | 0.79379 | 0.78353 | 0.77355 | 0.76385 | 0.75456 | 0.74462 | 0.73436
DLC from Kato 3 | 1.0286 | 1.3133 | 1.6754 | 1.7468 | 1.7249 | 1.6787 | 1.6205 | 1.5511 | 1.4701 | 1.3918 | 1.3221 | 1.2608 | 1.2051 | 1.1565 | 1.1136 | 1.0766 | 1.044 | 1.0143 | 0.98819 | 0.96293 | 0.94013 | 0.91982 | 0.90091 | 0.88221 | 0.86163 | 0.84384 | 0.828 | 0.81438 | 0.80269 | 0.79044 | 0.77908 | 0.76856 | 0.75881 | 0.74755 | 0.73781
DLC from Kato 4 | 1.0439 | 1.4838 | 1.7192 | 1.775 | 1.7514 | 1.6869 | 1.609 | 1.5257 | 1.4444 | 1.3674 | 1.2977 | 1.2362 | 1.1828 | 1.1364 | 1.0971 | 1.0612 | 1.0295 | 1.0017 | 0.97694 | 0.95374 | 0.93222 | 0.91135 | 0.89267 | 0.87529 | 0.85924 | 0.84433 | 0.83028 | 0.81667 | 0.80232 | 0.79032 | 0.78007 | 0.76978 | 0.76225 | 0.75368 | 0.74489

## Slide 3
DLC
CNe70 half coated
CNe13
StSt
Observe:
Half coated liner gives half e-cloud! Sharp edge! This means: coating => completely suppress e-cloud.
Three stripes on ECM. Did the magnet have 25 A? Check the magnet next time!

## Slide 4
Summary:
CNe70 half coated v.s StSt: half coated => half e-cloud
DLC: SEY = 1.8 StSt: SEY = 2.25 Low SEY => Low e-cloud
DLC conditions very fast. From -0.2 to -0.1 after one night scrubbing with 25 ns 4x72 LHC nominal beam.
StSt 50 ns v.s StSt 25 ns The difference: a factor of 3-5. The same as the earlier experimental results.

## Slide 5
Summary:
CNe 13 liner:
Has been in the SPS since Oct, 2008.
No ageing effect at all!

## Slide 6
Summary: e-cloud current for each supercycle as a function of beam intensity (protons/bunch)
4x72 with 25 ns bunch spacing:
No clear linear correlation saying that the e-cloud signal increases with increasing of beam intensity.
10 times higher e-cloud signal with 25 ns than 50 ns.
4x36 with 50 ns bunch spacing:
A weak tendency: e-cloud signal increases with increasing of beam intensity. (A big scattering?)
Giovanni:
E-cloud signal decreases with increasing of beam intensity?
Maybe?
No clear proof for it yet!
Chart: 
| 1.48 | 1.37 | 1.1800000000000002 | 1.1599999999999997 | 1.56 | 1.4 | 1.23 | 1.1379999999999997 | 1.1399999999999997
e-cloud current on StSt | 93347.12 | 108691.6 | 81724.56 | 71426.8 | 127401.68 | 90518.72 | 96770.88 | 84336.56 | 87764.16

## Slide 7
Chart: log(normalized current)
| StSt MD 3 (Oct, 2008) | StSt MD 8 (Nov, 2009) | CNe13 MD3 (Oct, 2008) | CNe13 MD8 (Nov, 2009) | StSt MD 9 (March 2010) | StSt MD 13 (Sept 2010)
25ns | -0.39794 | -0.60206 | -3.5229 | -4.699 | -0.39794
50ns | -1.0458 | -4.3979 | -4 | -4.7229 | -1 | -0.82391
75ns | -1.0969 | -4.699 | -4 | -5.5901