## Slide 1
Progress report on coatings for SPS-U
S.Calatroni, P.Chiggiato, P.Costa Pinto, M.Taborelli, I.Wevers,
C.Yin Vallgren, H.Pedroso-Marques, W. Vollenberg
Status of liner coatings
Testing programme
Proposal for installation
Status of SPS dipoles coating bench

## Slide 2: Liner status – lab testing
SPS test with liners:
  Old 2008 liner with carbon coating, exposed to air during shutdown
  Stainless steel liner for reference
  New liner with rough carbon coating (zirconium underlayer)
  A new slot is available. Proposal (to be discussed): carbon coating on getter underlayer
Sample in C-magnet:
  New sample holder being prepared

## Slide 3
Chart: Ageing of a-C film on SS samples, one curve each sample, on various zirconium underlayers
| 32 | 82 | 132 | 182 | 232 | 282 | 332 | 382 | 432 | 482 | 532 | 582 | 632 | 682 | 732 | 782 | 832 | 882 | 932 | 982 | 1032 | 1082 | 1132 | 1182 | 1232 | 1282 | 1332 | 1382 | 1432 | 1482 | 1532 | 1582 | 1632 | 1682 | 1732
CNe30_2_20090116_SS_1 | 0.83792 | 0.66517 | 0.74635 | 0.83339 | 0.88905 | 0.92206 | 0.9418 | 0.95144 | 0.95752 | 0.95707 | 0.95528 | 0.95346 | 0.9479 | 0.94325 | 0.93562 | 0.9297 | 0.92145 | 0.91493 | 0.90773 | 0.8989 | 0.89039 | 0.88103 | 0.87205 | 0.86292 | 0.85533 | 0.84616 | 0.83918 | 0.83204 | 0.82679 | 0.82033 | 0.81495 | 0.80811 | 0.80138 | 0.79795 | 0.79439
CNe30_3_20090116_SS_1 | 0.86532 | 0.61063 | 0.69278 | 0.7808 | 0.83993 | 0.88202 | 0.91265 | 0.93252 | 0.94603 | 0.95656 | 0.96342 | 0.96523 | 0.9647 | 0.96273 | 0.95977 | 0.95614 | 0.95205 | 0.9464 | 0.94059 | 0.93516 | 0.92951 | 0.92143 | 0.91348 | 0.90663 | 0.90069 | 0.89403 | 0.88818 | 0.88258 | 0.87765 | 0.87366 | 0.87056 | 0.86841 | 0.86715 | 0.86664 | 0.86814
CNe30_4_20090116_SS_1 | 0.84646 | 0.7436 | 0.80172 | 0.88293 | 0.93296 | 0.95868 | 0.97314 | 0.97855 | 0.97777 | 0.97514 | 0.97048 | 0.96583 | 0.9587 | 0.95251 | 0.9436 | 0.93504 | 0.92831 | 0.91966 | 0.91243 | 0.90319 | 0.8946 | 0.88496 | 0.87393 | 0.86507 | 0.85682 | 0.84667 | 0.83938 | 0.83118 | 0.82496 | 0.81824 | 0.81291 | 0.80621 | 0.80245 | 0.79862 | 0.79579
CNe30_5_20090116_SS_1 | 0.83618 | 0.76855 | 0.80339 | 0.88865 | 0.93471 | 0.96113 | 0.97361 | 0.97672 | 0.97596 | 0.97404 | 0.96991 | 0.96525 | 0.95909 | 0.95396 | 0.94629 | 0.9392 | 0.93234 | 0.92689 | 0.91919 | 0.91078 | 0.90261 | 0.89506 | 0.88549 | 0.87772 | 0.87058 | 0.86247 | 0.85474 | 0.84763 | 0.84052 | 0.83495 | 0.82989 | 0.82416 | 0.82056 | 0.81885 | 0.81925
CNe30_2_20090123_SS_1 | 0.83984 | 0.90901 | 0.78127 | 0.86436 | 0.91566 | 0.94406 | 0.9607 | 0.96945 | 0.97365 | 0.97397 | 0.97304 | 0.96959 | 0.96575 | 0.96046 | 0.95487 | 0.94909 | 0.94297 | 0.9364 | 0.92905 | 0.92221 | 0.91423 | 0.90607 | 0.89724 | 0.8888 | 0.87986 | 0.87216 | 0.86498 | 0.85861 | 0.85381 | 0.85362 | 0.85787 | 0.86275 | 0.86574 | 0.86725 | 0.86779
CNe30_3_20090123_SS_1 | 0.9559 | 1.0556 | 0.92131 | 1.015 | 1.0721 | 1.1098 | 1.1351 | 1.1497 | 1.1569 | 1.1568 | 1.1522 | 1.1458 | 1.1375 | 1.1294 | 1.1199 | 1.1102 | 1.1002 | 1.0905 | 1.0811 | 1.0718 | 1.0605 | 1.0488 | 1.039 | 1.0287 | 1.0194 | 1.0096 | 0.99926 | 0.9913 | 0.98703 | 0.98632 | 0.98674 | 0.98725 | 0.98776 | 0.98814 | 0.98797
CNe30_4_20090123_SS_1 | 0.87378 | 1.006 | 0.99714 | 1.0776 | 1.1113 | 1.1237 | 1.1223 | 1.1119 | 1.1002 | 1.0867 | 1.0701 | 1.0541 | 1.0425 | 1.0271 | 1.0138 | 1.0018 | 0.99003 | 0.97993 | 0.96958 | 0.95717 | 0.94744 | 0.93753 | 0.92458 | 0.91375 | 0.90313 | 0.89281 | 0.88471 | 0.87471 | 0.8717 | 0.86989 | 0.86775 | 0.86996 | 0.87123 | 0.8724 | 0.87329
CNe30_5_20090123_SS_1 | 0.9691 | 1.095 | 1.0118 | 1.0935 | 1.1333 | 1.1491 | 1.15 | 1.1426 | 1.1299 | 1.115 | 1.0988 | 1.083 | 1.0678 | 1.0529 | 1.0386 | 1.0253 | 1.0128 | 1.0012 | 0.9903 | 0.97895 | 0.96804 | 0.95655 | 0.94528 | 0.93429 | 0.92387 | 0.91428 | 0.90467 | 0.8951 | 0.88667 | 0.88104 | 0.8815 | 0.88357 | 0.8848 | 0.88569 | 0.88567
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Work is in progress, we have to understand some issues related to a-C layer uniformity and coating temperature

## Slide 4: Test on dual magnetron system, bldg 101
C source
Ti source
samples

## Slide 5: Ageing with Ti underlayer (getter for H2)
7 weeks in air
3 weeks in air
standard
Ti underlayer
4 days in air
Continuous Ti underlayer

## Slide 6: Proposal for 4th liner
Produce a NEG TiZrV underlayer on a liner
Assemble it in C coating system, activate NEG to pump H2 and perform standard carbon coating
Test samples in parallel

## Slide 7: MBB prototype test
MBB cross section; L=300mm; 2 rectangular carbon cathodes; Tested in LSS solenoids (B=190 Gauss)
B field

## Slide 8: MBB prototype test
MBB cross section; L=300mm; 2 rectangular carbon cathodes; Tested in LSS solenoids (B=190 Gauss)

## Slide 10
Cross section of the liner
L1
L2
R1
R2
Mid
Saved for aging
Sent to SEM for thickness measurement
 | δinitial onStSt | L1 | L2 | Mid
CAr9 – MBB2 | 1.03 | 1.03 | 1.03 | 1.06
CAr10 – MBB3 | 0.977 | 0.999 | 0.998 | 0.997
CNe31 – MBB4 | 1.03 |  |  | 
960 nm
630 nm
After 39 days in air: 1.07

## Slide 12: MBB coating bench in bldg. 867